## Slide 1: Effect of Fibre Properties on Processing Performance
Topic 27 – Lecture 1
(Greasy Wool to Top)

## Slide 2: Overview of Topmaking
Blend
Scour to remove grease, dirt, suint
Lubricate
Card to open up entangled wool and knockout the bulk of VM
Gill to remove hooks and to align fibres
Comb to remove neps, VM and short fibre
Gill to consolidate into an even sliver

## Slide 3: Mean fibre diameter of the top is set by the wool purchased (just 0.1 to 0.2µm coarser because more fine fibres are lost). Diameter distribution is set primarily by the CVD of the component lots unless a very wide range of D blended. Mean fibre length (H) is determined by staple length (SL) and breakage in processing. More breakage occurs for longer SL, for finer wool, for higher CVD and/or lower SS, and higher vegetable matter (VM) content. Higher % mid-breaks is also associated with shorter H. Lower curvature consistently gives rise to longer H (but the size of the effect is under dispute). Finer diameter, higher crimps/cm (higher curvature), lower SS and shorter SL are associated with more losses (noil) in combing.

## Slide 4: Fibre breakage in topmaking is primarily due to entanglement from scouring, any already in the fleece, or that associated with removing VM. There is limited scope for a given topmaker to alter the amount of breakage. Some gains can be made by reducing loads in carding and slightly longer H can be achieved by removing more short fibre. However, both reduce production and increase costs.

## Slide 5: The topmaker aims to meet the spinner’s specifications for the top at the lowest total price. The art is to purchase the most suitable lots in terms of price for performance which can be combined into a consignment that can be processed efficiently into the required top. The topmaker is particularly concerned to avoid problems or surprises in processing and freedom from contamination and faults of any form is always a requirement.

## Slide 6
Effect of Fibre Properties on Processing Performance
Topic 27 – Lecture 2
(Top to Yarn)

## Slide 7: Overview of Spinning
Re-comb top (particularly if dyed)
Gill (3 to 5 passages gradually thinning the sliver)
Rove (draft of 10 to 15 followed by rubbing or twisting to give strength)
Creel rovings on spinning frame and draft by 20 using double aprons and insert twist
Doff bobbins, steam, wind and clear
Two-fold for weaving or ply for knitting

## Slide 8: Sirolan-Yarnspec Top-to-Yarn Package “Best Commercial Practice” - Top properties ( D, H, CVD, BT..) - Yarn parameters ( tex, twist) - Processing conditions Yarn Properties & Spinning Performance
Notes: Theory and experiment have been combined into a software package (Sirolan Yarnspec) that aims to predict yarn properties and spinning performance. It aims to predict “best commercial practice” which is what a good mill should achieve if it doesn’t make any mistakes.
It uses the measured top properties (diameter, hauteur, diameter distribution, bundle tenacity and curvature [if available]), the yarn parameters (linear density and turns/m of twist) and the spinning conditions (size or rings, spinning speed, mass of traveller and whether re-combed or dyed top).

## Slide 9: Yarn properties can be well predicted
Source: Lamb and Yang (1998)
Notes: Excellent agreement is obtained between predicted and measured results for commercial mills. This figure shows a comparison of measured and predicted results for the unevenness of yarns (CV%) for leading Japanese and Italian mills.
A key reason that good predictions are possible is that everyone runs up against the statistical limit determined by the mean number of fibres in the yarn cross-section and that mills have similar machinery anyway.

## Slide 10: Relative importance of fibre properties 1. Mean diameter (µm) dominant 2. Hauteur (10mm = 1µm for spinning) 3. Strength (Δ10% = 6 to 9mm in H) 4. Diameter distribution (Δ5 in CVD% = 1µm) 5. Length distribution (CVH) over-rated
Notes: The excellent agreement between measured and predicted results gives us great confidence that we can state the relative importance of fibre properties and also know that there are not large unknown or unmeasured factors.

## Slide 11: Relative importance of fibre properties #2 Mean diameter determines the average number of fibres in the yarn cross-section, and hence evenness, strength and bending stiffness. 10mm extra fibre length gives an increase in yarn strength and spinning performance equivalent to that achieved by using 1µm finer wool. An extra 25mm of H is needed to match the improvement in evenness. Mean fibre strength (bundle tenacity - BT) can be important if there has been damage e.g. from dyeing, and a 10% drop in tenacity has a similar effect to a decrease of 6 to 9mm in H. However, BT is almost constant for undyed wools and only very weakly associated with staple strength.
Notes: The excellent agreement between measured and predicted results gives us great confidence that we can state the relative importance of fibre properties and also know that there are not large unknown or unmeasured factors.

## Slide 12: Relative importance of fibre properties #3 A wider diameter distribution has an effect similar to using a slightly coarser wool. To a good approximation a drop of 5 units in CVD% can be traded off against an increase of 1µm in mean diameter. Although many spinners put tight limits on hauteur distribution (CVH) there is little evidence that it affects processing although high values arise from more breakage in processing and extreme values can be generated by the Almeter if there is marked variation in along-fibre diameter. Yarns from wool with high curvature tend to be slightly less even.
Notes: The excellent agreement between measured and predicted results gives us great confidence that we can state the relative importance of fibre properties and also know that there are not large unknown or unmeasured factors.

## Slide 13
End of Summary Slides
Close Window