## Slide 1: Wool Carding Technologies
Topic 18
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: The woollen card
Uniform delivery of wool
Crushing of VM in web
Transfer and side-to-side mixing of web
Consolidation of separated strands (slubbing)
Two carding sections

## Slide 3: The worsted card
Burr beaters for VM removal
Feed hopper
Can coiler unit

## Slide 4: Feed control
Important to control rate of fibre delivery to card, especially for woollen carding
Mostly achieved by:
  Weigh pan
  Volumetric feed controlled by
    Weigh belt, or
    Beam of radiation

## Slide 5: Card clothing
Flexible wire (fillet)
  Wire staples inserted in flexible laminated backing
  Mostly used in woollen cards
  Requires fettling and grinding
Rigid metallic wire
  Continuous length of pressed steel
  Mostly used in worsted and semiworsted cards, also opening rollers of woollen cards
  No fettling or grinding needed

## Slide 6: Carding production
Maximise machine width (up to 3.5 metres)
  Used for woollen cards (condenser is bottleneck)
Increase overall machine speed
  Used for worsted cards
  Thibeau CA7 card
    2.5 metre wide, up to 220 kg/hr
    Other innovations included to optimise production

## Slide 7: Other factors effecting production and sliver quality
Carding yields – many factors (blend, settings,..)
Nep formation – fibre properties, card conditions
Use of automatic control systems
Maintenance requirements:
  Fettling – regular, only for woollen cards with fillet clothing
  Grinding – occasional, only for fillet clothing
  Cleaning, lubricating, check settings etc. - regular

## Slide 8
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen