## Slide 1: Industrial Environment & Practice
Topic 28
Judy Turk
Notes: This module looks at the current practice of Early Stage Processing and the impact of environmental issues
Produced for the CRC for Premium Quality Wool undergraduate program by Ms. J. Turk, Judy Turk Consulting.

## Slide 2: Components of ESP
Judy Turk
Greasy wool purchase
Creation of blends
Scour or Carbonise
Card
Gill
Comb
Finish Gill
Options:
    Machine Washable wool treatment
    Optim treatment
    High Lustre Treatment
    Soft Handle treatment
Notes: Written by: Ms. J. Turk, Judy Turk Consulting
Early stage processing is a term used to describe the wool processing activities listed on the slide.
Mills may be configured in many ways and this is just an example of common practice.
Some mills will only scour wool some only carbonise.
Some will not have treatments after combing, others will be what is termed a "vertical" mill and will take the wool from greasy to yarn or even fabric.

## Slide 3: ESP by-products
Woolgrease: when refined it is sold as Lanolin
Noil: Usually carbonised and used in felts or the woollen system
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
Valuable by-products are generated by the ESP industry.
Woolgrease is recovered from scour liquor and is used by pharmaceutical, cosmetic and manufacturing industries (eg paints, lubricants)
It undergoes refining up to the level required by the end user, the highest grade being BP (British Petroleum Standard)
ESP’s remove as much woolgrease as possible from scour liquors as it undesirable in effluent
2 Noil consists of the short fibres removed from sliver during combing.
As it is mainly the short fibres (some broken long fibres and kemps are also in the noil) it is finer than the parent wool, as a general rule the coarser the parent wool the greater the difference between the two mean fibre diameters.
It also contains the VM and neps that have been removed by the comb and a lot of Noil is carbonised before use in the woollen or felt industries.

## Slide 4: Scouring
Removes suint
Removes woolgrease
Removes dirt
 Achieves a clean, untangled product of white colour suitable for carding
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
The scouring process cleans the greasy wool.
It removes the suint, the substance secreted by the sheep which consists mainly of water soluble salts. Three stage scouring removes the suint prior to scouring, this improves the efficiency, wool quality and effluent management. Suint can be removed at a lower temperature (<40C), slightly higher pH (9) and with minimum use of detergent. If the suint is not removed prior to scouring at higher temperatures it may redeposit on the wool and become difficult to remove. Most of the dirt is also removed in the suint bowl.
The woolgrease is removed easily in a hot (60-66C) scour bowl with detergent. Woolgrease is liquid at about 40C and goes into solution with the scour liquor. The scour liquor is cycled through woolgrease extractors and is reused in the scour. As most of the dirt is removed in the suint bowl the quality of the woolgrease is improved. Recycling cleaned scour liquor saves on water and detergent use.
Scours need to be set up to avoid entanglement of fibres; if the wool becomes entangled, or worse felted, fibres will break in the card so reducing the value of the product.
Clean wool is necessary to run an efficient combing mill and to achieve efficient dyeing.

## Slide 5: Carding
Disentangles scoured wool to form a web (The sliver leaving a card consists of non-aligned fibres i.e. the fibres do not necessarily follow the direction of the sliver)
Breaks up and removes most vegetable matter (Small pieces of VM remain to be removed by the combs)
May form Neps that are removed by the combs
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
Both the woollen and worsted industries card the wool after scouring.
The worsted card is more vigorous than the woollen as the end product needs to be very aligned with less bulk. Woollen products are bulkier and retain all the short fibres.
Cards remove most of the VM but form neps (tangles of fibres ranging from <1mm to about 5mm). Small broken pieces of VM remain, many fall out during subsequent gilling and the last pieces are removed in the comb. Different types of VM cause different problems, clover type burrs may unravel, align with the wool fibres and become very difficult to remove. Shive type VM is difficult to remove because it will align with fibres and hard heads imbed in the card cloth causing down time for cleaning.
Card sliver is a web, ie the fibres are not aligned.

## Slide 6: Gilling
Gill machines align fibres so they run parallel to the sliver
Most combing mills will gill at least twice pre combing
Many mills gill three times
The same type of machines are used after combing to realign the fibres into a continuous sliver
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
The gills align fibres.
Card sliver is fed into the gills, they turn the card web into an aligned sliver but do not remove neps or VM.
A mill may be set up to run 2 or 3 gills, sliver direction is usually reversed between each gilling but some mills may “channel” their gills so the slivers are not run into cans but run straight through the gills, this process does not allow reversal of the sliver.
It is a belief that better quality and efficiency comes from reversing the slivers.

## Slide 7: Combing
Removes short fibres (Noil)
Removes most of the remaining VM
Removes most Neps
Combed wool is utilised in the worsted system
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
Combing is a very important part of the worsted system.
The comb can be set up to remove differing amounts of short fibre.
This setting is dictated by the quality required in the top.
If the setting is “close” less short fibres are removed and stay in the top. The mean fibre length will be shorter and the coefficient of variation of length will be higher, both attributes that affect the price and quality of the top. There will be less noil so the top can be sold cheaper than a top that is set up to remove more short fibres.
The end use and price of the top dictates the comb settings, the topmaker and spinner will negotiate this price. The topmaker will alter the blend to take this setting into account.
The settings and condition of the comb affect its efficiency at removing neps and VM.

## Slide 8: Carbonising
Wool is Carbonised to remove VM
Greasy wool is scoured prior to treatment
Acidification and baking the scoured wool removes VM by turning it into carbon
The carbon is crushed & dusted out
The acidic wool is neutralised
Carbonised wool is utilised in the woollen system
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk ,Judy Turk Consulting.
Carbonised wool is used in the woollen system
Wool is carbonised to remove VM.
Some sections of the industry do not want even very small amounts of VM in their product so will opt to use carbonised wool.
Oddments e.g. lox, bellies, crutchings, stains, pieces are carbonised but good quality lambs and fleece may also be used if required for specialty products.
The process:
Scour
Acidification
Drying
Baking
Crushing
Dusting
Neutralising
Bleaching (optional)
Drying

## Slide 9: Machine Washable Wool
The scales on wool fibres cause fibre entanglement
Entanglement (felting) causes shrinkage of wool products
To prevent shrinkage
Combed sliver is chlorinated which removes a portion of the fibre scales
Resin is added and coats the fibre to form a smooth fibre that will not felt
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
Wool does not shrink.
It felts because the scales which are along each fibre entangle with each other.
Felting occurs when agitation, moisture and heat are present; all of which occur in washing machines.
The process removes a small portion of each scale using, most commonly, chlorine then coats the fibre with a resin which bonds permanently to the fibre.
The fibre is then smooth and will not entangle during washing or wearing; as in dry felting.
Dry felting is commonly seen under arms of garments or in bedding; doonas or underlays.
This is why it is important that some products are machine washable even if it is planned to dry-clean them.

## Slide 10: Optim
Consumers of luxury goods require:
Fine fibre that is soft and does not prickle
Lustrous fibre in vibrant colours
The Optim process:
Stretches the wool fibre and reduces the diameter by at least 2 microns
Changes wool into a luxury fibre that is soft, lustrous and will dye to brilliant colours
It can no longer be called wool!
Judy Turk
Notes: Optim is a new fibre.
The process starts using wool but when finished it has a different profile ie the shape of the fibre is changed and it has quite different attributes.
Optim is used in the same market as cashmere or silk, it is a luxury fibre.
The fibre is made pliable then stretched, this reduces the mean fibre diameter by at least 2 microns and changes the cross section from round to flat sided.
The flat sides reflect light making the fibre lustrous, giving it different dyeing properties and because it so much finer it is extremely soft with no prickle.
It may be blended with wool or other noble fibres to create luxury goods.

## Slide 11: Environmental Issues
Pesticides in Greasy wool
Effluent management
Water Usage
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting
Australia has the “greenest” wool in the world but much of it still contains pesticides.
The European Union is at the forefront of environmental controls and as the EU is such a large market for wool it will dictate what the rest of the world does.
Currently 50% of Australian wool will pass the EU legislation but the limits are constantly being reduced so growers need to manage their flocks with this in mind.
Many customers who buy processed wool are still interested in “whole of life” environmental issues so even if the pesticides remain in Australia (in woolgrease or effluent) the customer sees it as a global problem and will not want the product.
Pesticides can be refined out of the woolgrease but this costs money and composting degrades the pesticides out of the effluent but the best option is to stop their use.
Customers are also interested in how much of the planets resources are used in processing so ESP’s must reduce the use of water and change chemicals to ones of acceptable bio-degradability.

## Slide 12: Environmental Legislation
EU The Water Framework Directive
EU The Integrated Pollution Prevention and Control Directive (IPPC)
Pesticide Limits in Greasy Wool
OC’s <0.5mg/kg (banned in Aust.)
OP’s <2mg/kg
SP’s <3mg/kg
IGR’s <2mg/kg
Exempt: Spinosad, Cyromazine, Dicyclanil
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, Judy Turk Consulting.
Legislation in the EU as it is at the moment 2004.
The limits will be reduced and controls will become stricter.

## Slide 13: Effluent Treatment
Each country and state will have differing legislation for effluent management
Wool scours have heavy effluent loads of mainly organic substances
When managed well organic substances can be recycled and the impact of a wool scouring industry on the environment is positive not negative
Judy Turk
Notes: Written by: Ms. J. Turk, Judy Turk Consulting.
Recycling of organic loads through composting and reuse of water are very cost effective and environmentally acceptable ways of managing wool scouring effluent.

## Slide 14
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen