## Slide 1: Wet Processing of Slivers, Tops and Yarns
Topic 25
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Wet processes for slivers and tops
Backwashing
Shrink resist treatment
Stretching of slivers and tops

## Slide 3: Backwashing
A sliver washing process, traditionally for removing dirt before Nobel combing
Now an optional treatment for enhancing the appearance of a top
  Removes dirt and processing lubricants
  Relax tensions on fibres introduced in carding, gilling, combing
Followed by gilling to restore fibre alignment

## Slide 4: Shrink resist treatment
Involves modification of wool fibre surface to reduce differential friction effect,
Hence propensity for felting is reduced
Chlorine-Hercosett Process:
  Chlorine treatment degrades scale edges, then
  Resin applied to cover scales
  Basis of easy care treatments for wool apparel, such as the Superwash systems

## Slide 5: Andar Superwash systems

## Slide 6: Sliver stretching processes
OPTIM Fine:
  stretching of wool top
  fibres permanently set
  produces finer, silk-like wool
OPTIM Max and lincLITE:
  Stretching and temporary setting
  Fibres blended with unstretched fibres for spinning
  When stretched fibres retract (in steam or water) produce bulking effect in yarn

## Slide 7: lincLITE process

## Slide 8: Wet processing of wool yarns
Scouring
Twist setting
Autoclaving
Insect resist
Antistatic treatment
Flame retardant application
Photo stabilisation
Stain blocking

## Slide 9: Yarn scouring
Washing treatment for removing processing lubricants, dirt etc. in woollen spun yarn
Methods:
  Dye-bath
  Tape scouring of hanks
  Package-to-package system (Twistset)
Other treatments (insect-resist, texturising also may be carried out)

## Slide 10: Tape scour conditions

## Slide 11: Stabilisation of yarn twist
Apparel yarns
  Autoclave setting for eliminating snarling
Carpet yarns – for superior appearance and appearance retention in use:
  Autoclave (steam) setting
  Boil set in dye bath
  Chemical setting (sodium metabisulphite) in
    Tape scour
    Twistset line

## Slide 12: Twistset system
The most advanced chemical setting system
Yarn wound off packages to form continuous blanket for processing
Transported through series of bowls:
  Bowl 1 – detergent scouring (60oC)
  Bowl 2 – MBS setting (85oC)
  Bowls 3, 4 – rinsing (85oC)
After drying, yarn rewound onto cones

## Slide 13: Twistset processing line

## Slide 14
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen