## Slide 1: Combing
Topic 11
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Objectives of combing
Remove short fibres from sliver before worsted spinning
Remove neps and vegetable matter fragments that will compromise yarn quality
Arrange fibres into parallel arrangement
Achieved by:
  Feeding sliver into comb
  Holding fibres and combing free end to remove short fibres
  Holding combed portion and combing previously uncombed fibres
  Forming continuous sliver of combed fibres from combed tufts

## Slide 3: Combing machines
Various types used in past
  Nobel (circular) – shown here
  Lister (nip motion)
  Holden (square motion)
Rectilinear combed mostly used today
  Intermittent action
  Up to 260 nips per minute
  Production: 24 – 36 kg/hr

## Slide 4: Rectilinear comb

## Slide 5: Combing sequence - feeding
Feed rollers A and feed gill B feed a fringe of fibres through the open nippers C and D

## Slide 6: Combing sequence – initial combing
Nippers C and D close
Fringe of fibres lower into pins of cylinder E
Penetration aided by brush F
Feed gill B moves back with feed grid R for next feeding cycle

## Slide 7: Combing sequence – final combing
Nippers CD open and shovel plate H moves forward
H supports fringe as top comb J descends
detaching rollers K draw fringe of fibres away

## Slide 8: Combing sequence - sliver formation
After drawing-off action complete…..
Carriage moves towards nippers
Detaching rollers recoil to start feeding out tail ends of previous fringe
As carriage apporaches nippers parallelisation controlled by air suction
New tuft of fibres overlapped over previous one by amount determined by desired thickness of delivered sliver
Sliver condensed by funnel, delivered to can

## Slide 9: Combing sequence - overview

## Slide 10: Final stages of topmaking
Finisher gilling
  Redistribute fibres in sliver to promote uniform drafting and cohesion
  Restore maximum fibre alignment, parallelisation
  Make linear density regular
  Provide further mixing
  Bring moisture content to required level
Packaging – ball top or bump top
Recombing – used mostly for dyed worsted tops or high quality tops
  Separate, align fibres, removes neps and short fibres
  Improves spinning and weaving efficiencies; yarn and fabric quality

## Slide 11: Combing production and quality
Measures of combing yield
  Tear ratio = mass of combed sliver/ mass of noil
  Noil(%)
Moisture content – regain
Combing quality – short fibre content affected by
  Raw wool characteristics
  Sliver properties (fatty matter level, regain)
  Quality of scouring, carding, combing
  Ambient temperature and humidity
  Comb setting

## Slide 12
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen