## Slide 1: Specification and quality of slivers and tops
Topic 23 – Lecture 1
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Key properties of slivers and tops
Mean fibre diameter **** (and variability **)
Mean fibre length *** (and variability **)
Colour ***
Coloured fibres ***
Vegetable matter **
Nep content **
Medullation *

## Slide 3: Modern instruments for fibre diameter measurement
OFDA
Source: BSC Electronics
Source: AWTA Ltd. (www.awta.com.au)

## Slide 4: Fibre diameter distribution
Mean fibre diameter

## Slide 5: Spinning limits for worsted yarns

## Slide 6: Importance of fibre length
Processing performance
  End breaks in spinning
  Weaving/knitting/tufting efficiency
Product quality
  Yarn strength and elongation
  Yarn evenness
  Fabric uniformity
  Fabric strength

## Slide 7: Almeter system for sliver fibre length measurement
Specimen preparation
Capacitance scanning

## Slide 8: Principle of the Almeter

## Slide 9: Almeter fibre length parameters
Hauteur fibre length distribution (numerical)
  Mean fibre length (mean hauteur)
  Short fibre content (eg, % fibres < 40 mm)
  Long fibres (eg, length exceeded by 5% of fibres)
Barbe fibre length distribution (length-biassed)
Mean fibre length (mean barbe) etc.
mean barbe > mean hauteur by ~ 25%

## Slide 10: Colour measurement
Colour determines the dyeing potential of the fibre
Measured by tristimulus values X, Y, Z where:
Y – an indicator of brightness (higher is better)
Y – Z an indicator of yellowness (lower is better)
Measured by colorimeters, spectrocolorimeters and spectrophotometers

## Slide 11: The effect of colour on dyeing

## Slide 12: Spectrophotometer – the main instrument for wool colour measurement
Wool sample in cell
Reflection grating
disperses light into
its components
Detector
AMPLIFIER
COMPUTER
X
Y
Z
Light source
Wool sample in cell
Reflection grating
disperses light into
its components
Reflection grating
disperses light into
its components
Detector
AMPLIFIER
COMPUTER
X
Y
Z
COMPUTER
X
Y
Z
Light source

## Slide 13: Other quality parameters for slivers and tops
Evenness
Coloured fibres
Foreign fibres
Neps
Vegetable matter
Residual grease
Dark Fibre Detector

## Slide 14: Specification and quality of yarns
Topic 23 - Lecture 2
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 15: Defining the construction
Count (or linear density) – related to thickness
  Direct system
  Indirect system
Number of plies
Twist
  Singles yarn (a ply)
  Folding twist

## Slide 16: Yarn count – direct method
Count (direct) is the mass of yarn in a specified length
Two common systems of units:
  Tex: 1 tex = 1 gram per 1000 metres
    1 Decitex = 1 gram per 10,000 metres
  Denier: 1 Denier = 1 gram per 9000 metres
The higher its tex or denier value, the heavier (and thicker) the yarn

## Slide 17: Yarn count – indirect method
Count (indirect): the length required to provide a specified mass of yarn
Many different systems used around the world – two widely used systems:
  Metric (Nm): no. of metres in 1 gram of yarn
  English Cotton (Ne): no. of 840 yard hanks in 1 pound of yarn
The higher the Nm or Ne value, the finer the yarn

## Slide 18: Folded yarns
Composed of two or more singles yarns, twisted together
Improves strength and uniformity of yarn, for
  ease of processing
  product appearance and performance
Yarns may be two-fold, three-fold, or occasionally a higher number of plies

## Slide 19: Twist
Staple fibres are twisted together to give strength and cohesion to a yarn (less important for continuous filament yarns)
The higher the twist, the tighter the fibres are locked together -> firm yarn
Measurement of twist: number of turns per metre of yarn
In folded yarns, specify both singles and folding twist

## Slide 20: Twist measurement methods
Untwist yarn until fibres parallel
Untwist then twist until pointer returns to zero mark

## Slide 21: Twist direction
Two alternative twist directions possible in spinning
  S twist and Z twist
Usual to have folding twist opposing singles twist to produce a stable yarn
  S on Z
  Z on S

## Slide 22: Yarn quality parameters
Strength
Elongation
Evenness
Hairiness
Bulk
Contamination
Moisture content
Twist retention

## Slide 23: Strength, elongation and recovery
Important for processing efficiency and product performance
Controlled mostly by fibre type (ie, strength, length, crimp) and yarn twist
Strength – the force (in Newtons N) required to break the yarn
Elongation (or extension) – the amount a yarn stretches before it breaks (expressed as % of its original length)
Recovery – how well the yarn returns to its original length after stretching

## Slide 24: Yarn evenness (or irregularity)
Important for manufacturing efficiency and product appearance
Influenced by fibre length and processing route (woollen yarns are least uniform)
Use Uster Evenness Tester to specify:
  Overall variation in thickness along yarn (CV)
  Periodic faults (occur at regular spacing)
  Frequency of thick or thin places
  Neps, slubs etc. per km

## Slide 25: Uster spectrograms of yarns
Yarn with no periodic variation in thickness
Yarn with significant periodic variation in thickness, as indicated by the prominent chimney

## Slide 26: Yarn hairiness
In an ‘ideal’ yarn all fibres follow a spiral path imposed by the twist
In practice some fibres protrude from the yarn surface, giving it a rough, hairy appearance
Hairiness is generally more prevalent in woollen spun yarns than worsted yarns
May be undesirable in apparel fabrics, because of prickle or inferior appearance
Worsted yarn
Singles - woollen
Two-fold - woollen

## Slide 27: Hairiness testing instruments

## Slide 28: Bulk
Bulk is the space-filling ability of a yarn
Bulky yarns tend to have a soft springy handle
Desirable for certain knitwear (and to give good resilience and ‘cover’ in carpets)
To maximise the bulk of yarns:
  Spin on the woollen system
  Use low level of twist
  Use highly crimped fibres (naturally or artificially produced)
  Dye yarn in hank form

## Slide 29: Yarn bulkometer
A pressure plate is applied to the yarn in the channel;
The mass of yarn in the channel is known (or can be calculated);
The volume occupied by the yarn is measured from the average height of the pressure plate (shown by arrows)

## Slide 30
End of Summary Slides
Close Window