## Slide 1: Overview of Wool Yarn Manufacture
Topic 2
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Major steps in textile processing
Carding
Staple fibres
Spinning
Twisting
Nonwovens
Knitting
Weaving
Tufting
Continuous filament
Texturising

## Slide 3: Spinning of staple fibres
Three alternative conventional routes
  Woollen system
  Worsted system
  Semi-worsted system
They vary in:
  The number of steps involved (complexity)
  The requirements for the raw materials (fibres)
  The characteristics of the yarns produced
  The end-products made from the yarns

## Slide 4: Common features of the systems
Carding (the most severe process on the fibres)
  Opens and disentangles the clumps of fibre
  Mixes the fibres
  Removes vegetable matter
  Arranges the fibres appropriately for the next stage
Spinning
  Inserts twist in the strand of fibres
  Produces an even, twisted strand of the required thickness
Twisting
  Combines two or more yarns together for strength

## Slide 5: Mechanical processing of wool
Sliver or slubbing formation - achieved by carding
  Disentangling and mixing fibres
  Removing vegetable matter
  Forming continuous web, sliver or slubbing
Preparing carded sliver for spinning (omitted from woollen spinning route) – achieved by gilling, combing and drawing
  Fibre alignment
  Evening
  Removal of short fibres, neps and other contaminants
Yarn formation
  Drafting
  Imparting cohesion through twist insertion
  Twisting for folded yarn, package formation,……

## Slide 6: Simplicity of the woollen route
Wool scouring
Blending and lubricating
Carding
Spinning
Scouring / Setting
Twisting
Coning
Loose stock dyeing
Hank dyeing
Blue indicates essential process
Red italics indicates optional process
Hanking (unless Twistset)

## Slide 7: Carding is achieved by the interaction of toothed rollers with the fibres
WORKING
STRIPPING
DOFFING

## Slide 8: Layout of a typical woollen card
Carder section
Condenser
Intermediate feed
Intermediate feed
Peralta rollers
Scribbler section
Feed hopper
Breast unit

## Slide 9: A woollen ring spinning frame
A singles yarn

## Slide 10: The worsted route has more steps:
Scouring
Blending
&
Oiling
Carding
Gilling (Preparing)
Combing
Gilling (Finishing)
Backwashing
TOPMAKING
SPINNING
Gilling (Drawing)
Roving
Spinning
Winding & Clearing
Twisting

## Slide 11: A worsted card for wool is more compact but has the same basic functions
Hopper feed
Can coiler
A thick rope of carded fibres, a sliver, is wound into a can for the next stage

## Slide 12: Functions of gilling
The front rollers rotate faster than the back rollers to draft the fibres
Back rollers
Front rollers
Lines of pins are pulled through the combined slivers to straighten and align the fibres
Multiple ends of sliver entering the gillbox together facilitate good fibre blending
By the drafting the gilled sliver exits with a lower linear density than the combined slivers entering the machine

## Slide 13: Combing
Most important step in the worsted process because:
  Separates long fibres (top) and short fibres (noils)
  Removes wool (or cotton) faults – neps, burrs and vegetable matter
  Waste material (noil) recycled back to woollen industry
  ~ 20 slivers fed simultaneously so get good blending too

## Slide 14: Drawing (or drafting)
In the worsted process a thick rope of fibres is drafted to a thin uniform strand, called a roving
Drawing may be performed by pairs of roller running at different speeds
Several drafting steps may be required to achieve the right roving thickness for spinning
Slow rollers
Fast rollers
Sliver in
Roving out

## Slide 15: Spinning
Ring spinning is the most common method, involving:
  Final drafting of roving down to thickness required in yarn
  Formation of yarn by insertion of twist
  Formation of yarn package on fast rotating spindle
Roving package
Drafting zone
(for thinning the roving)
Spindle (up to 17,000 rpm)

## Slide 16: Final steps in worsted spinning
Autoclaving or chemical setting eliminates tendency of yarn to ‘snarl’
Clearing involves automatically detecting and removing faults (thick or thin places)
Twisting combines two (or more) yarns to provide improved strength and evenness
The yarn is ready for weaving, knitting or tufting

## Slide 17: Worsted yarn characteristics
In comparison with woollen spun yarns, worsted yarns:
Have a very high level of fibre alignment with almost all fibres following the helical path imposed by twist
Hence they are very regular
Have very few fibre ends protruding from the yarn surface, so have a smooth feel and appearance
Have a low bulk and firm handle
Tend to be stronger (for similar twist and fibre length)
Minimum of around 40 fibres in yarn cross-section (compared to a lower limit of around 110 fibres needed for a typical woollen-spun yarn)

## Slide 18: Semiworsted spinning
A shorter version of worsted, without combing
Requires sound wool of good length with no vegetable matter
Produces a yarn with properties between woollen and worsted (smooth, even, strong)

## Slide 19
End of Summary Slides
Close Window