## Slide 1: Wool Coloration
Principles and Techniques
Topic 24
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Dyeing of wool
The application of colour to fibres, tops, yarns and fabrics
Can occur at several alternative stages in processing
Most water dyes are soluble in water
Dye molecule penetrates fibre and forms chemical bond with fibre

## Slide 3: Types of dyes for wool
Dye type | Shade range | Levelling ability | Wash fastness | pH range | Relative cost
Acid levelling | Bright pastels | Excellent | Poor | 2 – 3.5 | Cheap
Acid milling | Bright pastels | Poor | Very good | 6 – 7 | More than levelling
1:1 metal complex | Dull, dark | Good | Good | 2 | Moderate
2:1 metal complex | Dull, dark | Poor | Very good | 6 – 7 | More than 1:1
Reactive | Bright pastels | Poor | Excellent | 3 then 6-7 | Expensive

## Slide 4: Dyeing assistants
These are chemicals that promote:
Dyeing to the correct shade
Levelness
Colour fast results
Economical use of time, energy, dye
Minimal fibre damage

## Slide 5: Some examples of dyeing assistants
Antifoam agents
Buffer agents – to maintain optimum pH
De-aerating agents – releases air bubbles
Dispersing agents – smaller dye particles act more effectively
Exhaustion assistants – reduce time for dye to get ontl fibre
Levelling agents – promote level dyeings in 3 ways

## Slide 6: The 5 phases of dyeing
Dye molecules move towards fibre
Molecules attach to fibre surface
Molecules move into fibre
Molecules move in fibre or to another
Bonding of molecules

## Slide 7: Factors affecting dyeing
Fibre swelling
  Necessary to absorb water (and dye)
Polar groups in fibres (as in wool, cotton)
  Allow dye fixation by chemical means
Dye liquor interchange
  Moving goods and/or dye liquor
Temperature
Dye affinity
Chemical conditions
  pH, electrolyte concentration, auxiliary agents (such as retarding agents)

## Slide 8: 2 types of dyeing process
Exhaust dyeing
  Dye moves from dyebath into fibre in set time
  Used for: loose stock, hank, package dyeing,..
  Small to medium batch sizes
Continuous dyeing
  Goods pass through trough of liquor, sprayed, printed or foam dyeing
  Used for fabrics, carpets
  Large lengths of goods

## Slide 9: Loose stock dyeing
Dyeing of scoured wool before carding
Dye liquor circulated through stationary pack of wool
Subsequent blending gives level dyeing
Best suited to large lots of same shade
BUT
Some fibre damage reduces processing efficiency
Slower response to orders
Colour spinning requires more production planning

## Slide 10: Loose stock dyeing machine

## Slide 11: Hank dyeing
Yarn suspended in skein form on rods, immersed in moving liquor
More suitable for dyeing small amounts of yarn than loose stock dyeing
Enables yarn twist to be set, residual lubricant to be removed, maximum yarn bulk to be achieved
BUT
Accurate control of dyeing essential to achieve levelness

## Slide 12: Hank dyeing machine

## Slide 13: Package dyeing
Less handling, large batches
High rates of liquor circulation promote levelness
Amenable to automatic control
Low liquor-goods ratio give savings in water, effluent and energy
High temperature dyeing possible
Totally enclosed machinery promotes good working conditions

## Slide 14: Yarn package dyeing machine
Cones of yarn mounted on perforated tubes

## Slide 15: Top dyeing
Reasons for dyeing wool in top form rather than yarn
Several dye batches can be blended into a large batch by subsequent gilling
Batches of different colours can be blended to make mixed colour yarns
Shades that are difficult to dye evenly can be dyed then blended
Can carry stock of various shades in top form, for worsted spinning as required

## Slide 16: Top dyeing machine

## Slide 17
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen