## Slide 1: Ring spinning of yarns
Topic 12
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Preparation for spinning
Woollen spinning
  Slubbing from carding
Semiworsted spinning
  Sliver after 3 gillings
  Sometimes sliver is drafted to form a roving
Worsted spinning
  Top (gilled and combed sliver)
  Drawn (drafted and gilled) to form a roving

## Slide 3: Worsted drawing
Gilling of top
  Reduction in linear density
  Blending and regularising
  Fibre straightening
Drafting to form roving
  Reduction in linear density
  Improvement of strand strength/cohesion by rubbing or inserting twist
  Package formation
Production of rub roving

## Slide 4: Ring spinning spindle
Front rollers
Yarn guide
Drive
Package
Bobbin
Ring
Traveller
Ring rail
Ring rail movement

## Slide 5: The Traveller
A small clip that rotates around the ring at up to 45 m/s
Guides the yarn onto the bobbin
The heavier the yarn the heavier the traveller required

## Slide 6: Ring spinning machines
 | Worsted | Semiworsted | Woollen
Input material | Roving | Sliver (or roving) | Slubbing
Drafting system | Rollers + aprons | Rollers + aprons | Rollers
Draft | 15 – 30 | 80 – 120 | 1.2 – 1.3
Ring diameter | 45 – 65 mm | 75 – 180 mm | 100-300 mm
Spindle speed (rpm) | 7000-17000 | 3000-6000 | 2500-4000

## Slide 7: Woollen spinning frame
A low draft machine to handle weak strands (slubbings)
Features
  Slubbing delivered from spools
  Draft minimal: ~ 1.2 - 1.3
  Pneumafil tube sucks up broken ends
  False twist device gives cohesion to strand, aids drafting of fibres

## Slide 8: False twist device

## Slide 9: Worsted spinning frame
A high-draft machine to convert a very regular strand (roving) into a fine, smooth yarn for apparel
Features:
  Pairs of rovings drawn from package
  Drafting section: draft 15-30
  Wound onto package at 7,000 – 17,000 rpm

## Slide 10: Semiworsted spinning frame
Very high draft machine for converting sliver into yarn in one step
Double zone drafting devices often used
Used mostly for carpet and knitting yarns

## Slide 11
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen