## Slide 1: Principles of Wool Carding
Topic 9
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: The main functions of the card
Open and disentangle the blend to a single fibre state, with
  minimal fibre breakage and nep formation
  maximum yield and productivity
Mix the fibres to produce a very thin, even web
Remove impurities (dirt, dust, vegetable matter)
Deliver the fibres in an appropriate form to the next stage of yarn manufacture
  (i.e. slubbing for woollen yarn, card sliver for worsted and semiworsted)

## Slide 3: A simple card
Swift
Doffer
Fancy
Doffer comb
Worker
Stripper
Feed roller stripper
Angle stripper
Feed rollers
Feed sheet
Lickerin
Each roller is covered with special teeth, or clothing which is designed to fulfill a particular function (working, stripping, raising)
This diagram is a simplification of a full-size commercial card, which comprises two or more of these units placed end to end

## Slide 4: Functions of the card rollers
The feed sheet delivers the fibre to the feed rollers
The lickerin tears at the clumps of fibre leaving the feed rollers and there is some fibre breakage as partial separation of the fibre clumps occurs
The resulting tufts are carried to the fast rotating large cylinder, the swift via a transfer roller
A proportion of the fibre load on the swift is collected by a slowly-rotating worker, and eventually returned to the swift via a stripper roller
The fancy raises embedded fibres above the swift surface so that they may be caught by the doffer and transported to the next stage of the process.

## Slide 5: Working action – ‘Point-to-point’
A tuft of fibre is divided into 2 portions at a working point (between swift B and worker A)
One portion is captured by the worker, the other is retained by the swift
The fibres on the worker are returned to the swift (via the stripper) several seconds later
This delay provides a mixing effect
A
A
B
B

## Slide 6: Other actions
‘Point to back’ action – all the fibres are removed from one surface by a faster roller, as in stripping, with negligible fibre breakage
‘Back to back’ action – the raising action of the fancy roller
‘Point to point’ action – some fibres are retained by each surface, as in doffing (and working)

## Slide 7: Mixing on the card
The swift roller is the highway for wool travelling through a card
The worker roller diverts part of the wool flow and eventually returns it to the highway

## Slide 8: Mixing on the card
The doffer removes part of the flow
The workers temporarily divert the wool flow
Wool flow in
SWIFT
Wool not captured by doffer continues in the flow

## Slide 9: Smoothing effect of the card
A rapid change in input results in a slow change in output

## Slide 10: Fibre breakage on the card
A force is required to separate each fibre from its clump
If the force applied exceeds the fibre strength it will break
Excessive fibre breakage causes numerous problems
  Poor yields
  Spinning problems
  Weak and uneven yarns
  Pilling in fabrics; shedding in carpets
Fibre embedded in tuft
Separated fibre in web

## Slide 11: Tuft opening at the lickerin
A close-up view of the feed-roller/lickerin zone where initial tuft opening occurs
The fast-moving teeth of the lickerin tear away at the tuft as it is presented by the feed rollers

## Slide 12: Fibre capture by lickerin teeth
The fibre is pulled by the lickerin tooth until
One end is pulled free, or
The fibre breaks into two sections, or
The entire clump of fibres is pulled across onto the lickerin

## Slide 13: Fibre breakage at the lickerin
What determines which case occurs (free one end, break fibre or transfer entire clump?)
Fibre strength : how much tension can the fibre take before it breaks?
Force required to withdraw fibre from clump: depends on (a) degree of fibre entanglement, (b) fibre length and (c) friction between fibres
How firmly the clump is held by the feed rollers
Other factors also have some effect: roller speeds, tooth sharpness and angle, clearance between lickerin and feed rollers, fibre lubricant, etc.

## Slide 14: Effect of carding on fibre length
Factors affecting fibre breakage:
Fibre strength: depends on blend of fibres used, moisture content / extensibility
Degree of entanglement: introduced in scouring
Inter-fibre friction: controlled by lubricant addition
Restraining forces on fibre clumps: controlled by (a) feed roller clearances and (b) feed rate (thickness of mat of wool passing through feed rollers)

## Slide 15: Effect of original fibre length on fibre breakage
Source: Aldrich, Kruger and Turpie (1970)

## Slide 16: Hook formation in carding

## Slide 17: Nep formation in carding
Neps are tiny clumps of fibre produced by inadequate carding (eg, clothing wire too coarse to handle fibres)
Produce a thickness fault in the yarn unless removed by combing
Neps in card sliver
Neps in card web

## Slide 18
End of Summary Slides
Close Window