## Slide 1: Drafting and gilling of fibrous assemblies
Topic 10
Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Purposes of drafting and gilling
Reduce thickness of fibrous strand to that required for worsted and semniworsted spinning
Produce level of fibre straightening and alignment for spinning a smooth, even yarn
Also, by doubling, good mixing is achieved

## Slide 3: Drafting
The process of drawing out a sliver or roving to form a thinner strand
Usually carried out by rollers operating at different speeds
Calculated draft D = speed of front roller/speed of back roller
Actual draft D’ = input count / output count

## Slide 4: Doubling
The feeding of two or more ends into a drafting zone to promote
Mixing
Fibre alignment
Machine productivity
6 ends x 12 ktex
= 72 ktex
Draft = 8
1 end @ 9 ktex

## Slide 5: Causes of drafting problems
Fibres longer than the ratch setting may break due to stretch by the front roller
‘Floating fibres’ uncontrolled by either rollers can exit in bunches, producing drafting waves (periodic unevenness)
Ratch
Faster
Slower

## Slide 6: Methods of fibre control in drafting
Pin control (gilling)
Direct pressure control
  Carrier and tumblers
  Apron and tumblers
  Pairs of aprons
  Amblerdraft system

## Slide 7: Autolevelling
A control system which
Measures variations in sliver thickness
Alters the draft to reduce these variations
May operate mechanically (upper) or electronically (lower)

## Slide 8: Gilling (pin drafting)
Pinned bars (fallers) comb the sliver in the drafting zone
Provide fibre control in drafting
Straighten and align fibres
Faller driver mechanisms
  Screw gill
  Chain gill
  Pinned rollers

## Slide 9: Screw gill mechanism

## Slide 10: Chain gill mechanism
High production
Most common type of machine today

## Slide 11
End of Summary Slides - Close Window
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen